# Synthesis, Isolation and Structural Characterization of

# Some Metal-Carbides Metallofullerenes

(Title: Times, 14pt, Bold, Centered)

space>

○Takashi Inoue1, Yasuhiro Ito1, Hiroe Moribe1, Baopeng Cao1, Tetsuo Tomiyama1,

Toshiya Okazaki1, Toshiki Sugai1, Takako Suematsu2, Naoyuki Fujii2

Kazutetsu Nojima2 and Hisanori Shinohara1,3,4

(Author’s Name: Times, 12pt, Centered)

space>

1Department of Chemistry, Nagoya University, Nagoya 464-8602, Japan

2JEOL Ltd., Akishima, Tokyo 196-8558, Japan

3Institute for Advanced Research, Nagoya University, Nagoya 464-8602, Japan

4CREST, Japan Science and Technology Corporation, c/o Department of Chemistry,

Nagoya University, Nagoya 464-8602, Japan

(Author’s Address & Affiliation: Times, 12pt, Italic, Centered)

space>

Metal-carbide metallofullerene has been known as one of the new class of cluster endohedral fullerenes. (Sc2C2)@C84 is the first metal-carbide matallofullerene[1] which has been synthesized and structurally characterized by both 13C NMR and powder X-ray diffraction. At the first stage of the investigation, because the molecular formula (stoichiometry) of the fullerene was Sc2C86, this molecule had simply been considered as normal metallofullerene having a structure Sc2@C86. However, the (Sc2C2)@C84 structure with a Sc2C2 carbide cluster inside was clearly determined by 13C NMR and powder X-ray diffraction measurements. In this presentation, we report that one of the yttrium matallofullerenes, Y2C84(III), is a metal-carbide metallofullerene.

A 13C NMR spectrum of Y2C84(III) is shown in Figure 1. The spectrum exhibits in total 17 distinct lines that consist of a series of eleven full-intensity lines, five half-intensity lines and one 1/6-intensity line. Only C3v(8) isomer of IPR C82 can satisfy the number of NMR lines and relative intensity. We interpret that this metallofullerene has a metal-carbide endohedral structure in which two yttrium and two carbon atoms are encapsulated in the C82 fullerene, namely (Y2C2)@C82.

(Abstract: Times, 12pt, Left)

## space>

[1] C. R. Wang, T. Kai, T. Tomiyama, T. Yoshida, Y. Kobayashi, E. Nishibori, M. Takata, M. Sakata and H. Shinohara, Angew. Chem. Int. Ed., 40, 397 (2001).

(References: Times, 12pt, Left)

Corresponding Author: Hisanori Shinohara

TEL: +81-52-789-2482, FAX: +81-52-789-1169, E-mail: noris@cc.nagoya-u.a.jp

(Corresponding Author, TEL, FAX, E-mail: Times, 10pt, Left)